## Slide 1
Transforming CO2 and Sea Water to Green HYDROGEN & Green CEMENT Using Magnesium Waste Scrap
Rajesh Belgamwar, Sushma Rawool and Vivek Polshettiwar*
Department of Chemical Sciences, Tata Institute of Fundamental Research (TIFR), Mumbai, India
Email: rajesh.belgamwar@tifr.res.in, vivekpol@tifr.res.in
Introduction
Converting CO2 directly from the air to fuel under ambient conditions is a huge challenge. Thus, there is an urgent need for CO2 conversion protocols working at room temperature and atmospheric pressure, preferentially without any external energy input. Herein, we employ magnesium (nanoparticles and bulk), an inexpensive and the eighth-most abundant element, to convert CO2 to methane, methanol and formic acid, using water as the sole hydrogen source. The conversion of CO2 (pure, as well as directly from the air) took place within a few minutes at 300 K and 1 bar, and no external (thermal, photo, or electric) energy was required. Hydrogen was, however, the predominant product as the reaction of water with magnesium was favoured over the reaction of CO2 and water with magnesium. During CO2 conversion, Mg was converted to magnesium hydroxide and carbonate, which may be regenerated. Thus, even though the overall process is non-catalytic, it could serve as a step towards a sustainable CO2 utilization strategy.[1]
Objective
CO2 Reduction Experiment
CO2 Reduction: Kinetics, Productivity and Selectivity
Green Hydrogen Generation
Plausible Reaction Mechanism of CO2 Conversion
How to convert CO2 to fuel at room temperature and atmospheric pressure without any external energy?
Process Sustainability
Conclusions
CO2 (directly from the air or pure) was converted by magnesium (even scrap Mg) at room temperature and atmospheric pressure to methane, methanol, and formic acid, using water as the hydrogen source.
No external energy (such as light, heat, or electricity) was required.
The reaction was very fast, with a maximum product yield within 15 min.
This process produces 3.85 kg of green cement by mitigating 2.2 kg of CO2.
1 kg of Mg can produce 940 litres of green hydrogen, which is nearly 420 times more than the hydrogen produced by the reaction of Mg without CO2 (2.24 litre per kg of Mg).
Acknowledgement
We thank Infosys-TIFR for the travel grant. We also thank the Department of Atomic Energy, Government of India, and SHELL industries for funding.
References:
S. A. Rawool, R. Belgamwar, R. Jana, A. Maity, A. Bhumla, N. Yigit, A. Datta, G. Rupprechter and V. Polshettiwar. Chem. Sci., 2021,12,5774.
(a) PXRD pattern (TEM image as inset) of Mg.
(b, c) Methane yield as a function of reaction time for CO2 reduction by Mg NPs using, CO2 directly from the air and pure CO2
(d) Comparison of productivity of various metals and Mg–metal alloys.
(e) methanol, formic acid, and methane yields after 1h.
(f) methane, methanol, and formic acid yield quantified after 1, 5, and 15 min of CO2 reduction on Mg
Hydrogen yield with reaction time during CO2 reduction at room temperature and atmospheric pressure using water.
Reaction mechanism of CO2 conversion to methane, methanol, and formic acid by Mg using water.
Infosys-TIFR Fellow
CO2 conversion was carried out by taking 50 mg of Mg in a batch reactor and then sealed with a rubber septum.
CO2 gas was purged (50 mL min-1) into the batch reactor for 30 min for optimum CO2 adsorption on Mg surface.
Water was then injected into the reactor quickly in 20s under stirring, at room temperature and atmospheric pressure.
Reaction was initiated as soon as water was added.
The progress of the reaction was monitored by a online Micro GC.
Liquid products such as methanol and formic acid were identified and quantified by 1H NMR spectroscopy
(Experimental setup for Mg-assisted CO2 conversion.)
CO2 +H2O CH4 + CH3OH + HCOOH + H2
A direct conversion of CO2 to fuel,
at room temperature and atmospheric pressure
without the need for any external energy (no light, no electricity, no heat)
Just using water (no external hydrogen, even sea water works)
MAGNESIUM
0 to 25°C
(or air)
+ Mg-Basic Carbonate (Green Cement)
Magnesium converted CO2 (directly from the air or pure) at room temperature and pressure to methane, methanol, and formic acid, using water as the hydrogen source. No external energy (such as light, heat, or electricity) was required. The reaction was very fast, with a maximum product yield within 15 min.
This Mg protocol can even be used for H2 production (940 liter per kg of Mg), which is nearly 420 times more than H2 produced by the reaction of Mg with water alone (2.24 liter per kg of Mg)
“Green Hydrogen on Demand”
Portable Magnesium Cartridge which will produce H2 from Water and CO2 at Room Temperature and Atmospheric Pressure
H2O
CO2
Hydrogen
(a) 13C NMR spectrum of the reaction mixture (using labeled 13CO2) after 1 h of reaction of 13CO2 with Mg; (b) FTIR spectra, (c) PXRD patterns and (d) XPS C 1s spectra of solid products recovered after 1, 5, and 15 min of the reaction of CO2 with Mg
Economics of the Process
Life-Cycle Assessment (LCA)
*Preliminary (not comprehensive)
1 kg of Mg via simple reaction with water and CO2 produces in 1 hr,
Methane (2.43 lit),
Hydrogen (940 lit),
Mg-basic carbonate (3.85 kg),
Small amount of methanol, formic acid
This poster is just a model for reference. Only external dimensions are fixed, and the internal layout, fonts (style, size, color), line spacing, and colors are flexible and as per the author's preferences.